## Slide 1
End-of-waste criteria for
paper, glass, copper -
Main technical issues

## Slide 2: Key issues - paper
Possibility of end-of-waste for layered beverage cartons (BC)?
Draft Regulation:
End-of-waste comes with a restriction on the content of materials that cannot be recycled into paper or board: non-paper components ≤ 1.5%
The limit values covers:
  non-paper materials that can be separated from paper by dry sorting
  compound materials with a high content of non-paper materials (packaging board and paper sacks consisting of layers of paper and non-paper materials)

## Slide 3: Key issues - paper
Assessment of suitability for end-of-waste
- high content of non-paper materials (5-25%) such as plastics
separation of the non-paper materials takes place in special pulping processes,
in which non-paper residues are generated that require treatment and for which disposal is a common option
end-of-waste for unprocessed multi-material packaging would weaken the level of environmental protection

## Slide 4: Key issues - paper
Layered beverage cartons are currently waste and the fibres can effectively be recycled for their properties: good quality paper fibre, a value of aprox. 75 €/t.
The economics of recycling these fibres will not change substantially by end-of-waste for other paper grades.
In a few countries BC are collected with other paper (FI, SE, IT, IE), in most countries together with other packaging (DE, NL, BE, ES, FR, UK…), in any case with easy further separation.
Where BC are collected together with other paper, this practice does not need to change, and the material can be recycled within the waste regime.
Paper industry will continue to recycle fibres from layered BC.
Assessment of consequences for layered BC
Notes: .

## Slide 5: Key issues - paper
Possibility of end-of-waste for paper from multi-material waste collection?
The draft Regulation allows this possibility.
Assessment:
The high quality of EoW material will be ensured by the combination of the criteria:
  1.5% impurity threshold (non-paper components)
  Risky inputs and components are excluded: MSW, haz. waste, bio-waste, health care waste, oil, solvents, paint
  Treatments (such sorting, separating, cleaning, grading) shall have been completed.
In practice, only well-run treatment plants with advanced sorting techniques will be able to meet the criteria. This is expected to drive technology progress.
Notes: .

## Slide 6: Key issues – glass cullet
End-of-waste for glass cullet from cathode ray tube (CRT) waste?
The draft Regulation excludes this possibility:
Only waste from the collection of container glass, flat glass or lead-free tableware is allowed as input.
Mixed MSW, health care waste, hazardous waste are not allowed as input.
It has been proposed to allow end-of-waste for CRT glass cullet in order to avoid discrimination against other types of glass cullet
Assessment:
CRT waste is hazardous waste (high contents of lead, barium or strontium oxides)
When CRT waste is being recycled these metal oxides are not removed. Their content can only be reduced in molten state.
There is no demand for CRT glass cullet in the EU
Even without end-of-waste status CRT glass can continue to be recycled

## Slide 7: Key issues – copper and copper alloy scrap
Which limit value for foreign materials?
Draft Regulation:
The total amount of foreign materials shall be ≤ 2 by weight;
Foreign materials are:
(1) metals other than copper and copper alloys;
(2) non-metallic materials such as earth, dust, insulation and glass;
(3) combustible non-metallic materials such as rubber, plastic, fabric, wood and
other chemical or organic substances;
(4) slags, dross, skimmings, baghouse dust, grinder dust, sludge.
Assessment:
2% limit: keeps the direct environmental risks of scrap use low – supported by many Member States and the European copper industry
5% limit: more scrap would benefit from end-of-waste status, may lead to more collection of scrap but direct melting not always possible, higher emission levels without appropriate abatement – supported by scrap collecting and processing industry
Notes: .

## Slide 8: Key issues – monitoring
Stricter monitoring requirements?
Self-monitoring of impurities (foreign materials, non-paper components, non-glass components) in the draft Regulations:
Qualified staff shall carry out visual inspection of each consignment.
At appropriate intervals representative samples shall be analysed.
Frequency of sampling shall be established according to:
- The expected pattern of variability
- The quality of the input materials
- The precision of the monitoring method
- The proximity of results to the limit value
The process of determining monitoring frequencies shall be documented as part of the quality management system and shall be available for auditing
Proposal:
Prescription of a mass-based sampling method

## Slide 9: Key issues – monitoring
Assessment:
- Prescriptive approach may give the impression of more stringent control
- However, the variety of material grades, waste inputs and processing found in industrial reality is huge. Practically impossible or at least very costly to produce a reliable characterisation as a basis for a meaningful, i.e. sophisticated, prescription
- A simplistic prescriptive approach
  - would lead to over-testing or opting against end-of-waste in some cases
  - may serve as an excuse for under-testing in other cases
- It seems more meaningful to establish the appropriate monitoring frequencies and the sampling procedures for self-monitoring case by case.
- And to complement the self-monitoring by on the spot checks by the authorities

## Slide 10: Key issues – monitoring
Self-monitoring regarding hazardous properties in the draft Regulations:
- Qualified staff shall carry out a visual inspection of each consignment.
- The staff shall be trained on how to recognise the relevant potential hazardous properties.
- The procedure of recognizing hazardous materials shall be documented under the quality management system.
- Where visual inspection raises any suspicion of possible hazardous properties, further appropriate monitoring measures, shall be taken.
Concern raised:
- Visual inspection might not be sufficient to ensure that end-of-waste criteria are met

## Slide 11: Key issues – monitoring
Assessment:
- Hazardous waste shall not be used as input, except (only in the case of Cu scrap) where proof is provided that it has been treated to remove all hazardous properties
- Systematic chemical composition analysis would put a substantial additional burden on the system. Today chemical composition analysis is needed and done by users for technical/commercial reasons. Not for environmental reasons.
- Waste processors judge on the properties of their materials based on knowledge of the input materials, the processing applied and relying on the expertise of their staff.
- Spot checks by authorities may include chemical analysis.